**Raw Data**

**Proliferation assay of three different MWs of chitosan combined with 0.024 µg/mL OPG concentration using 3D culture system**

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Viability percentages | | |  | standard deviation | | |
|  | A | B | C |  | A | B | C |
| 24 | 98.5 | 89.2 | 91.3 |  | 8.3 | 20 | 25.5 |
| 48 | 110.2 | 101 | 104 |  | 9.6 | 17 | 16.2 |
| 72 | 203.9 | 169 | 173.4 |  | 17 | 22.5 | 9.1 |