

Image Name: NiS2#1952-1\_HP2

Image Resolution: 1024 by 768

Image Pixel Size: 1.61 µm

Acc. Voltage: 15.0 kV

Magnification: 80



Weight %

|  |  |  |
| --- | --- | --- |
|  |  ***S*** |  ***Ni*** |
| ***Amostra2b(3)\_pt1*** |  51.62 |  48.38 |

Atom %

|  |  |  |
| --- | --- | --- |
|  |  ***S*** |  ***Ni*** |
| ***Amostra2b(3)\_pt1*** |  66.15 |  33.85 |