

Image Name: NiS2#1928-2\_HP2

Image Resolution: 1024 by 768

Image Pixel Size: 1.98 µm

Acc. Voltage: 15.0 kV

Magnification: 65



Weight %

|  |  |  |
| --- | --- | --- |
|  |  ***S*** |  ***Ni*** |
| ***Amostra2b(2)\_pt1*** |  52.56 |  47.44 |

Atom %

|  |  |  |
| --- | --- | --- |
|  |  ***S*** |  ***Ni*** |
| ***Amostra2b(2)\_pt1*** |  66.98 |  33.02 |