


Image Name: NiS2#1928-2\_HP

Image Resolution: 1024 by 768

Image Pixel Size: 0.26 µm

Acc. Voltage: 15.0 kV

Magnification: 499



Weight %

|  |  |  |
| --- | --- | --- |
|  | ***S*** | ***Ni*** |
| ***Amostra2b(1)\_pt1*** | 53.07 | 46.93 |

Atom %

|  |  |  |
| --- | --- | --- |
|  | ***S*** | ***Ni*** |
| ***Amostra2b(1)\_pt1*** | 67.44 | 32.56 |