|  |  |
| --- | --- |
| **Samples** | **Mean** |
| Control, light, DI water | 7.17±0.06 |
| 4A+ beads, light, DI water | 7.13±0.06 |
| Control, dark, DI water | 7.20±0.00 |
| 4A+ beads, dark, DI water | 7.13±0.06 |
| Control, light, tap water | 7.27±0.06 |
| 4A+ beads, light, tap water | 8.40±0.10 |
| Control, dark, tap water | 7.27±0.06 |
| 4A+ beads, dark, tap water | 6.43±0.06 |