Supplementary Information

Hydrogen production by photocatalysis using new composites based on SiO2 coated by TiO2

Werick Alves Machado,1,2. Antonio Eduardo da Hora Machado1,3

1Universidade Federal de Uberlândia, Instituto de Química, Laboratório de Fotoquímica e Ciência de Materiais, Uberlândia, Minas Gerais, Brazil

2 Instituto Federal de Educação, Ciência e Tecnologia do Triangulo Mineiro (IFTM), Ituiutaba, Minas Gerais, Brazil

3Universidade Federal de Catalão, Unidade Acadêmica Especial de Física, Catalão, Goiás, Brazil

Tables

| Table T1- Rietveld refinement reliability factors |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Photocatalyst | Rb | Rf | Rwp | Rexp | S |
| W50 | 1,17 | 0,78 | 11,0 | 9,46 | 1,16 |
| W50S25 | 2,82 | 1,05 | 11,7 | 9,85 | 1,18 |
| W50S50 | 2,13 | 1,13 | 16,8 | 12,8 | 1,31 |
| W50S75 | 4,23 | 1,74 | 19,0 | 13,8 | 1,37 |

Figures

a) a) Figure S1- a) Images obtained by SEM; b) EDS spectra and c) particle size distribution histograms for the W50 photocatalyst. c) c) b) b) a) a) Figure S2- a) Images obtained by SEM; b) EDS spectra and c) particle size distribution histograms for the W50S25 photocatalyst. c) c) b) b)

a) a) Figure S3- a) Images obtained by SEM; b) EDS spectra and c) particle size distribution histograms for the W50S50 photocatalyst. c) c) b) b) a) a) Figure S4- a) Images obtained by SEM; b) EDS spectra and c) particle size distribution histograms for the W50S75 photocatalyst. b) b) c) c) a) a) Figure S5- a) Images obtained by SEM; b) EDS spectra and c) histograms of particle size distribution for silica. c) c) b) b)

Figure S6- Nitrogen adsorption / desorption isotherms obtained for synthesized oxides: a) W50, b) W50S25, c) W50S50, d) W50S75 and e) SiO2.

Figure S7- Diffractograms obtained after refinement Rietveld for the following photocatalysts: a) W50, b) W50S25, c) W50S50, d) W50S75.

Figure S8- Raman spectrum of pure SiO2.