Table 5 Effects of Representative Flame Retardants on Mechanical Properties of PC/ABS Alloys

| Flame-Retardant System | Representative Retardant | Loading (wt%) | Impact Strength (kJ/m²) | Change Rate | Tensile Strength (MPa) | Change Rate | Key Influencing Factors |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Unmodified | - | - | 45.0 | - | 58.0 | - | - |
| Halogenated | TBBPA/Sb₂O₃ | 15 | 28.5 | ↓36.7% | 46.5 | ↓19.8% | Brittle Sb₂O₃ phase |
| Organophosphorus | BDP | 10 | 38.2 | ↓15.1% | 52.3 | ↓9.8% | Plasticizing effect |
| Inorganic Phosphorus | Microencapsulated red phosphorus | 14 | 30.1 | ↓33.1% | 43.8 | ↓24.5% | Red phosphorus agglomeration |
| Silicone-Based | Polymethylphenylsiloxane | 8 | 41.3 | ↓8.2% | 55.6 | ↓4.1% | Flexible siloxane chains |
| P-Si Synergistic | RDP + nano-SiO₂ (9%+5%) | 14 | 36.8 | ↓18.2% | 50.2 | ↓13.4% | Weak interfacial bonding of SiO₂ |
| P-Si Compound | DPA-SiN | 30 | 22.5 | ↓50.0% | 38.7 | ↓33.3% | Phase separation at high loading |
| P-N Synergistic | APP/PER (22%+8%) | 30 | 24.8 | ↓44.9% | 36.9 | ↓36.4% | Rigid structure of PER |